Geiger-mode devices for charged particle tracking
J. Trenado1, O. Alonso1, A. Comerma1, M. Vos2, E. Vilella1, L. Garrido1 , A. Dieguez1
1UB Barcelona, 2IFIC Valencia
December'12
Juan Trenado jtrenado@ecm.ub.es
IX Jornadas de Futuros Colisionadores

---
OUTLINE
Introduction
Avalanche Photodetector in Geiger-Mode.
Machine Background in ILC-CLIC.
Device behaviour vs thicknes and detection threshold.
First prototype for Test Beam
APD Matrix 43x10
Previous Test Beam
Noise Characterization: Noise and Crosstalk
TB Simulations
Test Beam
Setup: CNM trigger and Mechanics
Problems and solutions
Operating Mode: Gating
First MIP detection
Conclusions

---
Introduction - Avalanche Photodetectors in Geiger-Mode
Diode biased above the breakdown voltage.
Linear Mode: Biased below the breakdown. Electrons provoke multiplication. Lineal response, proportional to the incident radiation.
Geiger Mode: Biased above the breakdown. Electron and holes provoke multiplication. Binary response.
Linear Mode
Geiger Mode

---
Occupancies
Introduction - Machine Background in ILC-CLIC
Density of Hits/BX in a) ILC b) CLIC
Hits/mm2/BX
Hits/mm2/BX
M. Vos et al., Forward tracking at the next e+e- collider, part II (in progress)
	CLIC / [Hits/Pixel/BX]	ILC / [Hits/Pixel/BX]
VXD	2·10-5 - 2·10-6	6·10-5 - 5·10-7
FTD	2·10-5 - 2·10-7	3·10-7 - 2·10-8
SIT		3·10-7 - 8·10-8
APD Dark Counts (Vop=21.2V; Tobs=30ns): 2.6·10-5 / With overlapping
Occupancy due to Dark Counts is the same order than the machine VXD

---
Introduction - Device behaviour vs thicknes and detection threshold.
Ultra-thin sensors give rise to low-multiplicity clusters, that will imply smaller pixel occupancy.
CLIC Background Studies and optimization of the innermost tracker elements Dannheim, D. et al. Proceedings LCWS11, arXiv:1203.0942 [physics.ins-det]

---
First prototype for Test Beam
APD Matrix 43x10 pixels. Pixel size: 20x100 μm
First Prototipe in AMS 350nm. Single devices without electronics and array of 8 pixels with quenching resistor and follower integrated.
First Prototipe in ST 130nm. Single devices and array.
First Prototipe for TB: AMS 350nm.

---
Previous TB – Noise Characterization
4% of noise with overlaping means less than 1 pixel with DC.

---
Previous TB – Crosstalk Characterization
Optical Crosstalk and Diffussion
Electronics
Electronics
?
Pixels in the same
row share the n-tub
Optical Crosstalk
Avalanche

---
Previous TB – Crosstalk in the Same Well
Pixels in the same row share the cathode. Charge from hit pixel can diffuse until its neigbour.
We measure a crosstalk level between neighbouring pixels sharing the same well of 2% (tobs=30ns and Vop=21.2V)

---
Previous TB – Optical Between Wells
Pixels in different row have electronics between them. An avalanche emit photons that can be absorved by a neighbour pixel.
Optical crossstalk is compatible with 0.

---
Previous TB – TB Simulations
Simulations performed with Geant4.
Setup composed by
2 Aluminum layers, 100um thickness.
2 Silicon blocks for APD matrix, 250um thickness
1 Silicon block for trigger device, 300um thickness.
20μm
Multiple scattering has a sub-micron contribution to the telescope precision for SPS runs at CERN. Internal structures like guard rings (1.1μm thickness) can be characterized.
At DESY and Bonn the precision (~10 um) permits to obtains global efficiencies.
100μm

---
Test Beam – Setup: CNM Trigger
Diode as a trigger based in a Neutron Detector.
Portable Silicon Neutron Detector System
C. Guardiola, J.Rodríguez, C. Fleta, D. Quirion, M. Lozano
Proceedings of the 8th Spanish Conference on Electron Devices, CDE'2011

---
Test Beam – Setup: Mechanics
Developed and aligned in Valencia.
Alignment between DUTs and trigger using metrologic optical method.
Thanks to J.V. Civera.

---
Test Beam - Operation Mode
Oscar is working to reduce toff to 700ns.

---
Test Beam - Problems and Solutions
One of the two matrix we carried out broke down before the
begining.
The die unsticked from the PCB and the wirebondings supported the chip.
The matrix showed a short circuit in three lines.
With just one matrix we could not remove noise by overlapping. To obtain low level noise we had to work with short observational time and low overvoltage.
We worked with tobs=30ns and Vov=21.2V
APD ran 4 hours with a rate of 5%. We did not have time to resolve the problem of the low rate. The statistic obtained is poor, local eficiencies will not be measure.

---
Test Beam - First MIP detection
Correlation between the APD matrix and the MIMOSA sensors.
We are trying to analise the data to obtain the efficiency althougth the poor statistics.
APD sees MIPs!!!!

---
Conclusions
Test Beam
APD devices are capable to observe MIP at low overvoltages.
The Test Beam in CERN was succesful in the goal to observe MIPS, the problems happened made not possible to make measures of local efficiencies with high statistics.
Next TB will be in autumn in DESY, there is the posibility of make a TB in Bonn in spring.
Precision in Bonn-DESY will permit measure global eficiencies.
Irradiación.
Literature explain that total reverse saturation current is not resposible of dark counts due to superficial current. It is not possible to make a direct deduce of the effects of irradiation. We expect low increment in DC. Would be interesting to irradiate APD with the dosis for ILC, step by step.
We had to consider make a new run in APDs AMS 0.35um to perform succesfully the activities during the next year
Improvements
The PCB of the matrix and the FPGA will be redisign to improve mechanical matching and remove low impedance path.
The BUSY signal will be redisign to reduce the dead time.
The trigger will be change for a bigger one for a better fit with the matrix.
Posibility to use ATLAS-FEI4 in Bonn
A second setup will be build.