## Slide 1: Accelerator technology for Higss Factory
C. Oliver, F. Toral (CIEMAT)
Jornada Red Futuros Colisionadores – 2nd July 2024

## Slide 2
e- Source
e+ Main Liinac
e+ Source
e- Main Linac
Damping Ring
Beam dump
Interaction point
Physics Detectors
Bunches of ~1010 e+/e-
What is this talk NOT about?
Neither accelerator overviews nor a comparison…
… but it is about CIEMAT contribution to accelerator technology for potential future colliders
No physics
No detectors

## Slide 3: Ongoing activities on accelerator technology for future colliders at CIEMAT
C. Oliver, F. Toral (CIEMAT)
Jornada Red Futuros Colisionadores – 2nd July 2024

## Slide 4
PRISMAC program
Facilities
CIEMAT contribution to:
HL-LHC
FCC
ILC
CLIC
Conclusions
Outline
18 short and long nested superconducting (SC) orbit correctors
16 T dipole in common coil configuration
Conduction cooled SC magnet package
Dipole with longitudinally variable field (permanent magnet) and RF structures

## Slide 5: Collaboration with CERN: PRISMAC program
PRISMAC PROGRAM : A CIEMAT-CDTI Collaboration for Research on High Field Magnets, Supported by SGI/MCI & CERN

## Slide 6
Facilities: magnet laboratory
We are working on the commissioning of a new laboratory for prototyping magnets up to 2 m long and 10 ton. Overall surface about 900 m2.
  Underground: mechanical workshop, laser cutting machine, storage
  Ground floor: winding area, reaction furnace, dimensional control room, collaring press, magnetic measurement bench, assembly
  First floor: offices

## Slide 7
Facilities: superconductivity laboratory
2 vertical cryostats for liquid helium
Assembly hall with 3 cryocoolers
We can test magnets both in vertical cryostats or using cryocoolers. The superconductivity laboratory is at CEDEX premises (Julián Camarillo, Madrid).

## Slide 8
CIEMAT contribution to HL-LHC

## Slide 9
MCBXF is an orbit corrector magnet located in the Inner Triplet, the closest group of magnets to the interaction points. Inner Triplet will be upgraded for HL-LHC.
View of LHC and IP5 with location of IT magnets
MCBXFB
(2.5 T∙m)
MCBXFA
(4.5 T∙m)
Inner Triplet Corrector Package
CIEMAT contribution to HL-LHC: MCBXF
Vertical dipole field
(2.1 T)
Horizontal
dipole field (2.1 T)
Combined
dipole field
(Variable orientation)

## Slide 10: Magnet layout
MCBXF Technical specifications | 
Magnet configuration | Combined dipole (Operation in X-Y square)
Integrated field | 4.5 (A) / 2.5 (B) Tm
Minimum free aperture | 150 mm
Nominal current | < 2000 A
Radiation resistance | 35 MGy
Physical length | < 2.5 (A) / 1.505 (B) m
Working temperature | 1.9 K
Iron geometry | D1 (A) / MQXF (B) iron holes
Field quality | < 10 units (1E-4)
Fringe field | < 40 mT (Out of the Cryostat)
    Coil fabrication techniques not previously used due to the high number of turns.
Up to 147 kNm/m ¡¡~140 times the electric Porsche Taycan Turbo S motor torque!!
First nested superconducting accelerator magnet with mechanical torque locking
Courtesy L. Bottura (CERN)
CIEMAT contribution to HL-LHC: MCBXF

## Slide 11
Nested H/V dipoles
150 mm single aperture
Nb-Ti technology
Integrated field: 4.5 T.m (A), 2.5 T.m (B)
Two lengths with the same cross section:
  Type A (2.5 m long)
  Type B (1.5 m long)
Courtesy of J.A. García Matos
Deliverable: “bare” magnet
  Collared coils within yoke, longitudinal and transverse loading system
  Integration in cold mass at CERN
  Powering Tests done in CERN
CIEMAT contribution to HL-LHC: MCBXF
MCBXFB: Short magnets
  Two prototypes (MCBXFBP1, MCBXFBP2) at CIEMAT facilities
  Series of 12 magnets
MCBXFA: Long magnets
  Prototype (MCBXFAP1) at CIEMAT facilities
  Series of 6 magnets

## Slide 12
Nested correctors MCBXF: coil production at CIEMAT
  NbTi Rutherford cable insulated with braided glassfiber
  Double pancake coils: binder
  Impregnated with CTD 101K resin
  Two lengths: 1.5 and 2.5 m
Binder mould assembly
Impregnation mould assembly
CIEMAT contribution to HL-LHC: MCBXF

## Slide 13
Mag. Measurements of the Inner Dipole
HL-LHC: Nested corrector magnet assembly at CERN
Dipoles, endplates and iron laminations
Inner Dipole Assembly
Outer Dipole in press
Both Dipoles with End Plates
Outer Dipole in assembled
Magnet ready to be transported to Test Station
Assembled in collaboration with CERN (927 laboratory)

## Slide 14
CIEMAT contribution to FCC

## Slide 15
CIEMAT contribution to FCC:
16 T dipole in common coil configuration (
Initial constraints for the research on high field magnets at CIEMAT:
  Some delay in starting the activity due to the workload driven by MCBXF magnets.
  The new laboratory will not be fully operational till end 2024.
  Previous work was focused on common coil layout.
Our strategy is based on the following steps:
  Model magnet using ERMC coils in common coil configuration.
  Revisit the existing design of 16T common coil dipole magnet.
  Research on fabrication techniques: react-and-wind coils.
  Prototype of a high field magnet in common coil configuration.
R&D on High Field Magnet

## Slide 16
ISAAC: Model magnet using RMC coils
Motivation:
  The main challenge of high field common-coil dipoles is mechanics
  We can test different support structures with existing coils
ISAAC: Investigating Superconducting Assembly to Address Common coil mechanics

## Slide 17
Motivation:
  The main challenge of high field common-coil dipoles is mechanics.
  No need to produce Nb3Sn coils at CIEMAT laboratory.
Strategy:
  Calculation of a model magnet in common coil configuration using existing RMC coils: magnetic, mechanical, protection.
  Engineering design: 3D model, fabrication drawings, tooling.
  Fabrication of components.
  Assembly at CERN (927 workshop): training on bladder and key technology. Most of assembly tooling is available.
  Test at CERN (SM18).
Model magnet using RMC coils

## Slide 18
Motivation:
  16 T is too challenging for our first high field magnet.
  Adapt the design to the procured cables.
Strategy:
  Define the input parameters: properties of procured cables, main dimensions, main field objective.
  Calculations: electromagnetic, mechanical, protection.
  Engineering design: 3D model, fabrication drawings.
Revisit the existing design of 16T dipole
Motivation:
  Possible cost-effective solution of series production of high field magnets.
  Common coil layout is the only one compatible with this technique.
Strategy:
  Analysis of past experiences.
  Calculation of a model coil and evaluation of the feasibility of a model magnet.
  Engineering design: 3D model, fabrication drawings, tooling.
  Fabrication.
  Test at CERN (SM18).
React and wind coils

## Slide 19
CIEMAT contribution to ILC

## Slide 20
SC Quadrupole package at the center of the cryomodule (B) of the SRF string for beam acceleration
Quadrupole magnet combined with dipole corrector and BPM (IFIC)
Conduction cooled to avoid the need of a He cryostat
National MAGNEXT Project: design, fabrication and characterization of conduction-cooled coils with large temperature margin (in collaboration with KEK).
ILC: conduction cooled magnets (MagNext)

## Slide 21
CIEMAT contribution to CLIC

## Slide 22
Variable high field magnets
Manufacturing of Power Extraction and Transfer Structures (PETS)
RF structure manufacturing
CIEMAT CONTRIBUTION TO CLIC

## Slide 23
Development of dipole magnets with variable longitudinally field based on permanent magnets: low-emittance damping rings.
CLIC: permanent magnets

## Slide 24
TD26CC
CLIC: RF structures
Disks manufactured by Spanish Industry (EGILE)
Tolerances fully achieved
Pending RF tests at CERN

## Slide 25
All the ongoing projects on accelerator developments for future colliders drive substantial innovative aspects for our group.
High temperature superconductors are not included in the ongoing projects, but we are in conversations with the Spanish funding agency CDTI to start this activity.
We are working on different technologies for three future collider proposals: FCChh, ILC and CLIC.
Spanish (CIEMAT) accelerator contribution to future colliders should not be exclusively “magnets”
Very close contact with Spanish industry.
Conclusions