## Slide 1
V. Rollano*, A. Gomez, A. Pascual, M.C. de Ory, D. Rodriguez,
D. Granados, J. Martín-Pintado,
on behalf of the CADEx colaboration
*vrollano@cab.inta-csic.es
Centro de Astrobiología (CSIC-INTA), Spain
IMDEA Nanociencia
November 19th
The CADEx experiment: progress on the technology demonstration of the superconducting Kinetic Inductance Detectors (KIDs)

## Slide 2
Motivation
Superconducting Lumped Element Resonators (LERs)
Implementation
Results
  Setting the operational frequency band
  Dark cryogenic characterization
  Radiation absorption characterization: responsivity to W-band
Summary

## Slide 3
Motivation
Superconducting Lumped Element Resonators (LERs)
Implementation
Results
  Setting the operational frequency band
  Dark cryogenic characterization
  Radiation absorption characterization: responsivity to W-band
Summary

## Slide 4
Looking for axions in the mm/submm/Far- IR desert
Novel detection system:
Haloscope + KIDs
Motivation

## Slide 5
Motivation
Superconducting Lumped Element Resonators (LERs)
Implementation
Results
  Setting the operational frequency band
  Dark cryogenic characterization
  Radiation absorption characterization: responsivity to W-band
Summary

## Slide 6
Superconducting Lumped Element Resonators (LERs)
LERs as Kinetic Inductance Detectors (KIDs)
Superconducting detectors for mm/submm astronomy

## Slide 7
Superconducting Lumped Element Resonators (LERs)
LERs as Kinetic Inductance Detectors (KIDs)
Superconducting detectors for mm/submm astronomy

## Slide 8
Superconducting Lumped Element Resonators (LERs)
  High quality factor  Low losses
  Low noise  High sensitivity
  Frequency-multiplexable
  Frequency and geometry tunability
WHY LERs?

## Slide 9
Motivation
Superconducting Lumped Element Resonators (LERs)
Implementation
Results
  Setting the operational frequency band
  Dark cryogenic characterization
  Radiation absorption characterization: responsivity to W-band
Summary
Notes: -This is the outline of my talk.
- I will start by briefly introducing the concept of a superconducting lumped element resonator (LER).
-Then, I will explain the development process, including design, fabrication and characterization.
- afterwards, I will discuss some notable results of my thesis. Both, in the field of astronomy detectors and quantum processors.
At the end, I’ll finish with a quick summary of my presentation.

## Slide 10
FABRICATION
CHARACTERIZATION
DESIGN
Implementation
Notes: - Firts, we design the resonator geometry

## Slide 11
Hybrid quantum system on a chip
Tuning operational frequency band: Pixel Geometry
LEKID  Inductor = Absorber
Matching impedance:
Solid absorber:
Z0 =Zeff
l/20 > s
Geometry  Polarization sensitivity
Free Space
Z0=377 W/sq
Zeff
Implementation
Notes: The other promissing application is use these LERs as Kinetic Inductance Detectors (KIDs), for astronomy.
KIDs are a very promising type of superconducting detectors in which every pixel, couple to a single transmission line consist of a microresonator at a specific resonant frequency.
They working princpiple is that the incidence of photons with energy higher tan the superconducting energy gap  breaks cooper pairs on the superconductor  producing a change in the kinetic inductance, and, therefore, a mesurable change in the resonance.
(Physically, this is because a smaller number of carriers must have a greater velocity than a larger number of carriers in order to achieve the same current).

## Slide 12
Resonance frequency
Coupling quality factor
Quality factor Q
Internal quality factor
LER Parameters
Impedance Z
Microwave Electromagnetic Simulations
Implementation

## Slide 13
CHARACTERIZATION
DESIGN
FABRICATION
Implementation

## Slide 14
LERs nanofabrication in Clean Room
Sputtering / Electron beam evaporator:
Deposition of superconducting films
Nano and micro lithography
Laser writer
Focus ion beam
ISO 4
Superconducting layer: Ti/Al
Resist
Etching:
Wet etching, ion milling and RIE
Stripper:
Removing the resist
Acetone bath
Oxygen plasma
Substrate
Implementation

## Slide 15
DESIGN
FABRICATION
CHARACTERIZATION
Implementation

## Slide 16
Radio-Frequency Characterization set-up
He3/He4 Dilution Refrigerator
Characterization

## Slide 17
Motivation
Superconducting Lumped Element Resonators (LERs)
Implementation
Results
  Setting the operational frequency band
  Dark cryogenic characterization
  Radiation absorption characterization: responsivity to W-band
Summary

## Slide 18
M. C. de Ory et al. , IEEE TMTT (2024)
High internal quality factor:
Kinetic fraction:
Dark cryogenic characterization
Results
High superconducting film quality
High nanofabrication yield
9 pixels demostrator
Notes: Revisar distancia al backshort
Inductor: strip grating
  Width = 3 µm
  Gaps = 440 µm
Impedance Matching:
  Distance between LEKIDs 𝓁2 = Si/2 = 483 µm.
  Backshort at the rear side of the BiKID structure 𝓁1= 300 µm.
LEKID area  2 at the absorption frequency

## Slide 19
  Proximity Effect: Titanium/Aluminum bilayers
2
15 nm Ti (Tc 0.4 K )
15 nm Al (Tc 1.2 K )
Ti Thickness
Setting the operational frequency band to the W-band
Results
2
  W-band : 75-110 GHz  Ti/Al suitable
A. Catalano et al., A&A (2015)
Ti/Al:
  Impedance Matching
LEKID  Inductor is the effective optical absorbing área  Geometry constrains
T=100 mK

## Slide 20
Radiation absorption characterization
responsivity to W-band
Results
Blackbody temperature controls optical loading
Filter Stack
TBB (1 K– 7K) : Optical Power Load
Notes: -

## Slide 21
Radiation absorption characterization
responsivity to W-band
Results
(rad)
Notes: -

## Slide 22
Radiation absorption characterization
responsivity to W-band
Results
Frequency noise response
FFT
Two Level Systems Noise
Notes: -

## Slide 23
Radiation absorption characterization
responsivity to W-band
Results
Frequency Noise Equivalent Power
Background limited
Two Level Systems Limit

## Slide 24
Characterized LEKIDs noise response sweeping the Black Body temperature.
Best NEP is about . We are still background limited.
Sensitivity is close to the baseline of CADEx
Forward to achieve the CADEx goal
TLSs reduction and 1/f noise mitigation
Responsivity measurement improvements in a controlled low background environment.
Summary

## Slide 28
Hybrid quantum system on a chip
Kinetic Inductance Detectors (KIDs)
Cooper pairs density
ns
2
Quasiparticle density
nqp~0
PHOTON  Ephoton>2Δgap
ns
Absorbed photon
Change in…
SUPERCONDUCTING PROPERTY
Cooper pairs density
n's <ns
2
Quasiparticle density
n'qp >nqp
?
LK
KINETIC INDUCTANCE
Notes: The other promissing application is use these LERs as Kinetic Inductance Detectors (KIDs), for astronomy.
KIDs are a very promising type of superconducting detectors in which every pixel, couple to a single transmission line consist of a microresonator at a specific resonant frequency.
They working princpiple is that the incidence of photons with energy higher tan the superconducting energy gap  breaks cooper pairs on the superconductor  producing a change in the kinetic inductance, and, therefore, a mesurable change in the resonance.
(Physically, this is because a smaller number of carriers must have a greater velocity than a larger number of carriers in order to achieve the same current).

## Slide 29
Hybrid quantum system on a chip
Capacitor
Inductor
LK
nCP
Day et al., Nature (2003)
We can detect
incident power
by monitoring
the shift in f0
L=Lg+Lk
Kinetic Inductance Detectors (KIDs)
Notes: The other promissing application is use these LERs as Kinetic Inductance Detectors (KIDs), for astronomy.
KIDs are a very promising type of superconducting detectors in which every pixel, couple to a single transmission line consist of a microresonator at a specific resonant frequency.
They working princpiple is that the incidence of photons with energy higher tan the superconducting energy gap  breaks cooper pairs on the superconductor  producing a change in the kinetic inductance, and, therefore, a mesurable change in the resonance.
(Physically, this is because a smaller number of carriers must have a greater velocity than a larger number of carriers in order to achieve the same current).

## Slide 30
Transmission line
Multiplexing  1 wire > 1000 LERs
Multiples LERs coupled to a single transmission line
KIDs:
1 read-out wire
>1000 pixels
Kinetic Inductance Detectors (KIDs)
Notes: -They present the great advantage that they are intrinsically multiplexable, as we can couple many resonators with it characteristic resonance frequency, couple to the same transmission read out line, allowing for compact resonators geometries.
-For example, changing the capacitor finger length, we can chan the capacitance, and so that the resonance frequency from one LER to another.
-
-They present the great advantage that they are intrinsically multiplexable, as we can couple many resonators with it characteristic resonance frequency, couple to the same transmission line, allowing for compact resonators geometries.
-For example, changing the capacitor finger length, we can chan the capacitance, and so that the resonance frequency from one LER to another.
-𝐵:𝑡𝑜𝑡𝑎𝑙 𝑐𝑎𝑝𝑎𝑐𝑖𝑡𝑜𝑟 𝑤𝑖𝑑𝑡ℎ;𝐿_𝑐:𝑓𝑖𝑛𝑔𝑒𝑟 𝑙𝑒𝑛𝑔𝑡ℎ