## Slide 1
CHARGE AND SPIN SENSING
AT THE SINGLE PARTICLE LEVEL
M. Fernando Gonzalez-Zalba
Ikerbasque Professor / CIC nanoGUNE
Principal Quantum Engineer /Quantum Motion
Notes: Semiconductor spin qubits are a great physical platform for quantum computing, but one of its outstanding challenges its readout. It remains it slowest computational step but there is a lot of potential to do better. Over the course of the last couple of years, we have done some really nice work towards ameliorating this problems that I would like to share with you.

## Slide 2
quantum hardware
We develop silicon-based quantum computing hardware
Areas of coverage
Spin qubits in silicon quantum dots
Cryogenic electronics
Spin qubit device modelling
Intelligent Automation of quantum processors
Hardware-aware quantum algorithms
Packaging
Notes: Thermal modelling and signal integrity

## Slide 3
Quantum Motion team
Executive team
People & Operations
Quantum Hardware
Cloud Engineering
IC Design
IC Validation
Device Modelling
Packaging
Cryogenic Labs
Intelligent Automation
Quantum Algorithms & Theory

## Slide 4
WELCOME TO VISIT US
fernando@quantummotion.tech

## Slide 5
Outlook
Charge and spin readout at the single particle level
Topics:
Silicon electron spin qubits
The readout challenge
Progress on rf readout of spin qubits
Single-electron transistors (Superinductors)
Single-electron boxes (Tunable and HMM)
In-situ dispersive readout (rf cascade style)
Notes: Particularly, I have 3 exciting results, each focusing on one of the three types of sensing techniques that are available for semiconductor spin qubits.

## Slide 6
Electrical readout of SPINs
Measuring the spin of a single electron is an extremely hard task
- Spin-selective optical excitation
- Magnetic resonance force microscopy
- Direct electrical readout is complex
Spin-to-charge
conversion
Charge
detection
Kolbe electrometer
Elzerman et al, Nature 430 431 (2004)
Notes: Since it is the first talk of the session and the workshop, you would allow me to evangelize for a little bit about silicon spin qubits and why they are a great system to work with.
The qubit, the spin of a single electron in isotopically enriched silicon is one of the most coherent solid-state system in nature with coherence on excess on 20 ms. This is, the quantum memory time that approaches the time our laptop memories retain information for (DRAM memory).
And recently, it has been demonstrated that spins can be operated at elevated temperatures of the order of 1.5K, which puts them in an ideal place to be interfaced with low-power cryogenic electronics.
Coincidentally, the devices that have been used to demonstrate this phenomenal physical properties, look very much like transistors.

## Slide 7
Electrical readout of SPINs
Measuring the spin of a single electron is an extremely hard task
- Spin-selective optical excitation
- Magnetic resonance force microscopy
- Direct electrical readout is complex
Spin-to-charge
conversion
Charge
detection
Kolbe electrometer
Spin sensitivity:
10 spins/sqrt(Hz)
100 seconds to detect 1 spin
Charge sensitivity:
<10-5 electrons/sqrt(Hz)
100 picosecond to detect 1 electron
Bienfait et al, Nat Nano 11 253 (2016)
Thomas et al, Nat Electron 8 75 (2025)
Notes: Since it is the first talk of the session and the workshop, you would allow me to evangelize for a little bit about silicon spin qubits and why they are a great system to work with.
The qubit, the spin of a single electron in isotopically enriched silicon is one of the most coherent solid-state system in nature with coherence on excess on 20 ms. This is, the quantum memory time that approaches the time our laptop memories retain information for (DRAM memory).
And recently, it has been demonstrated that spins can be operated at elevated temperatures of the order of 1.5K, which puts them in an ideal place to be interfaced with low-power cryogenic electronics.
Coincidentally, the devices that have been used to demonstrate this phenomenal physical properties, look very much like transistors.

## Slide 8
Silicon SPIN QUBITS
Can be operated at elevated temperatures
Fidelities close to fault tolerant thresholds at 1.4K
Beneficial for integration with classical electronics
Yang et al, Nature 580 350 (2019)
Coherent transistor-like devices
M Veldhorst et al, Nature Nano 9 981 (2014)
One of the most coherent solid-state systems (T2 = 28 ms)
Enabling 1Q, 2Q gates well beyond 99%
Notes: Since it is the first talk of the session and the workshop, you would allow me to evangelize for a little bit about silicon spin qubits and why they are a great system to work with.
The qubit, the spin of a single electron in isotopically enriched silicon is one of the most coherent solid-state system in nature with coherence on excess on 20 ms. This is, the quantum memory time that approaches the time our laptop memories retain information for (DRAM memory).
And recently, it has been demonstrated that spins can be operated at elevated temperatures of the order of 1.5K, which puts them in an ideal place to be interfaced with low-power cryogenic electronics.
Coincidentally, the devices that have been used to demonstrate this phenomenal physical properties, look very much like transistors.

## Slide 9
Scaling spin qubits
Repeated unit cell
Two-dimensional arrangement with NN
Necessitates classical electronics
Requires frequent readout
O(1M) qubits
The Surface Code
A silicon CMOS image sensor
Repeated unit cell
Two-dimensional arrangement
Integrates diodes and classical electronics
O(10M) pixels read at 30 fps
O(100M) pixels
Notes: When thinking how to build a useful quantum computer using these technology, we need to think of fault-tolerant operation. For that, we look at the error correction algorithm of the surface code, the most error-forgiving algorithm, that sets some guidance on how a quantum processing unit may need to look like to deliver such capability.
It's based on a repeated unit cell, in a two-dimensional arrangement. It will need to be integrated with classical electronics for control and readout and it is likely that thousands to millions of qubits will be required to provide utility.
Luckily for us working with semiconductors, such requirements remind very much of one of the most advanced technologies, that of the silicon CMOS technology and in particular, CMOS image sensors. They consist of a repeated unit cell, the pixels, with two-dimensional arrangements, integrated diodes and electronics and reaches the complexity of several hundred million pixels in sufficiently small footprint such as it fits in your pocket.
For that reason, may researchers like me, see silicon as the technology that will take us there.

## Slide 10
Repeated unit cell
Two-dimensional arrangement with NN
Necessitates classical electronics
Requires frequent readout
O(1M) qubits
The Surface Code
Repeated unit cell
Enables 3(4)xN arrays today
Integrates readout electronics
Readout is slowest and breaks the connectivity
O(1M) qubits?
Silicon planar MOS technology
Scaling spin qubits
Notes: A CMOS quantum processor today can achieve some of these requirements, we are able to make repeated unit cells. With great 3D fabrication techniques pioneered at HRL now 3 or even 4xN arrays of quantum dots can be manufactured with integrated readout, but it is those sensors, that present a challenge being readout the slowest step and having a large physical footprint that breaks qubit connectivity.

## Slide 11
Repeated unit cell
Enables 3(4)xN arrays today
Integrates readout electronics
Readout is slowest and breaks the connectivity
O(1M) qubits?
Silicon planar MOS technology
Scaling spin qubits
Can we address some of the readout challenges?
Making sensors faster
Exploring compact versions
Notes: A CMOS quantum processor today can achieve some of these requirements, we are able to make repeated unit cells. With great 3D fabrication techniques pioneered at HRL now 3 or even 4xN arrays of quantum dots can be manufactured with integrated readout, but it is those sensors, that present a challenge being readout the slowest step and having a large physical footprint that breaks qubit connectivity.

## Slide 12
OUR APPROACH
Work with silicon fabs to enable large integration
IMEC’s 300 mm line
Multi-gate MOS process
GlobalFoundries
Integration of Analog, Digital and Quantum Electronics
Notes: Our approach towards silicon spin qubits at quantum motion has been to utilise industrial manufacturing to enable large scale integration, and over the course of this talk, you will see results coming from our two fab partners, IMEC primarily for the qubit work and Globalfoundries for the cryoCMOS and the readout peripherals.

## Slide 13
R. Li et al. IEEE IEDM 9371956 (2020)
200 nm
GB0
G0
G1
GB1
Silicon mos qubits
Notes: Focusing today on IMEC, let me guide you through how we make qubits in this MOS platform.

## Slide 14
QUBITS
Overlapping gate design
3-layer process (polysilicon gates + SiO2)
Plunger, barrier and confinement gates
Isotopically enriched silicon (29Si - 800 ppm)
Low charge noise gate stack < 0.5 μeV/√Hz
Physical Gate yield > 99%
C. Laine et al, arxiv:2505.10435 (2025)
R. Li et al. IEEE IEDM 9371956 (2020)
QUBITS
200 nm
GB0
G0
G1
GB1
RESERVOIR
SENSOR
Silicon mos qubits
Notes: We use a 3 layer metal gate process (poly plus silicon oxide) on isotopically enriched silicon.
We can create quantum dots where to isolate single electron spins. We can create QD charge sensors next to. And have electronic reservoirs from where to get the electrons loaded.
The interface is very quiet with low levels of charge noise and devices are reliable with gate yields above 99%.

## Slide 15
Key characteristics:
Impedance matched for amplification with a HEMT – High bandwidth
Absorbs energy when driven at its resonant frequency
Changes in device impedance (due to a charge sensing event) produce a change in the magnitude of the reflection coefficient (as well as a change in Q)
Schoelkopf et al, Science 280 1238 (1998)
200 nm
The rf single-electron transistor
Impedance matching
Notes: The sensor: we will normally hook up a single electron transistor (a sensing quantum dot) to a matching network for amplification with a HEMT transistors, providing this way high bandwidth readout. The setup absorbs energy when driven at its resonant frequency and both the magnitude and phase of the voltage change when a charge sensing event occurs in its vicinity.

## Slide 16
Spin readout
Multi-chip assembly
Superconducting spirals – to minimise losses
Parallel topology – to control coupling
DQD Tune up and Pauli Spin Blockade
For spin to charge conversion
~(2,0)
~(1,0)
~(2,1)
~(1,1)
(NL,NR) = (# e- in left QD, # e-in right QD)
P1 (V)
P2 (V)
Notes: For many of us, in practice this looks like a multichip assembly with superconducting spirals to minimise losses and help achieve better coupling. Then we tune up our QD to the 31-40 charge transition where we are going to do our spin projections, and particularly as we move from 31 to 40 spin-dependent transitions occur, Pauli spin blockade.

## Slide 17
Multi-chip assembly
Superconducting spirals – to minimise losses
Parallel topology – to control coupling
17
DQD Tune up and Spin Readout
Even
Odd
,
,
,
Readout time = 10 us
Fidelity (Parity) >99%
Spin readout
Notes: In ptactice this leads to two possible measurement outcomes, for odd and even parity spin states, which we can comfortably read in 10 us with fidelity in excess of 99%.

## Slide 18
Multi-chip assembly
Magnetically-driven ESR
Visibility > 99%
Superconducting spirals – to minimise losses
Parallel topology – to control coupling
Spin readout

## Slide 19
Can we do better?
What should we ask from a readout sensor?
High fidelity – well above 99% for error correction
The dream: The fastest and highest fidelity step while compactly integrated on chip
Fast – faster that the relaxation and coherence times
and IDEALLY not the slowest computational step
Compact – small on-chip footprint including peripheral electronics

## Slide 20
Rf readout
Dissipative
Charge sensing (SET, QPC)
Dispersive
In-situ (DGS)
Charge sensing (SEB)
Vigneau et al., App Phys Rev (2022)

## Slide 21
Rf readout
Dissipative
In-situ (DGS)
Charge sensing (SEB)
Vigneau et al., App Phys Rev (2022)
Largest on chip footprint
Based on Resistance Changes
Indirect measurement
Most sensitive to date
Smallest on chip footprint
Based on Capacitance changes
Direct measurement
Lowest sensitivity
Intermediate on chip footprint
Based on Capacitance changes
Indirect measurement
Intermediate sensitivity
Dispersive
Charge sensing (SET, QPC)
Compatible with MUXing Techniques

## Slide 22
Rf readout
Large resistance swings
Large coupling to dot
Good matching
High Z
Manage rf losses
Large gate charge
Tunnel rate matched to rf
Large coupling to dot
High Z,Q
High frequency
Good matching
Manage loss & parasitic caps
Large gate charge
Tunnel coupling matched to rf
High Z, Q
High frequency
Good matching
Manage loss & parasitic caps
Device
Resonator
RF management
Vigneau et al., App Phys Rev (2022)
Dissipative
In-situ (DGS)
Charge sensing (SEB)
Dispersive
Charge sensing (SET, QPC)

## Slide 23
Spin qubit readout
Dissipative charge sensing (SET)
Integrated superinductor
Non-linear
T, Swift et al. arxiv:2507.13202 (2025), review Nat Electron
C. Laine et al. arXiv:2505.10435 (2025) in Nat Sensors
Dispersive Charge Sensing (SEB)
A tunable single-electron box
3 state classification (HMM)
Chittock-Wood et al. arxiv:2408.01241 (2024), in Nat Electron
In-situ Dispersive Readout
New rf cascade method
A two-qubit gate
Notes: Superinductor
SEB results
Models
Cascade

## Slide 24
Dissipative charge sensing

## Slide 25
Integrated readout using a superinductor
in 22FDX technology
Swift et al. arXiv:2507.13202 (2025)

## Slide 26
Superconducting inductor on a separate chip
(+) Easy to quickly prototype, good sensitivity
(-) Not scalable, lack of reproducibility
Integrated superconducting inductor?
TiN thin films superconductor below 1 K
Ultra-dense kinetic inductance ~1 nH/sq
Noah et al. App Phys Rev (2024)
A superinductor
26
Tom Swift

## Slide 27
Inductor size downscaling
x35,000 enhancement in inductance density
Integrated superconducting inductor?
TiN thin films superconductor below 1 K
Ultra-dense kinetic inductance ~1 nH/sq
Swift et al. arXiv:2507.13202 (2025)
A superinductor
27
Tom Swift
Noah et al. App Phys Rev (2024)

## Slide 28
Resonant Circuit for testing
Confirms resonant behaviour of inductor
Lk1(2)=130(170) nH for L=50µ and w=0.36n
Enables determining Lk wrt to system params
Dependent on T, B, DC and AC current
Kinetic inductance follows theory expectations
Impedance -> Superinductor
Swift et al. arXiv:2507.13202 (2025)
RESONANT, NON-LINEAR INDUCTOR
28
Tom Swift

## Slide 29
Integrated circuit
Results
Reflection coefficient dependent on transistor impedance
Coulomb diamonds
Mimics DC current response
Including:
Superinductor & capacitors
QD-transistor
INTEGRATED RFSET
29
Tom Swift

## Slide 30
Integrated circuit
Including:
Superinductor & capacitors
QD-transistor
RFSET: SENSITIVITY
30
Tom Swift
Signal boost in the non-linear regime rather than
Possibility to exploit the superconducting-to-normal phase transition
Sensitivity improvement
We find a SNR=2600 in 4 ns equivalent to tmin = 1 ps.
Improvement over >x500 wrt the state-of-the-art*
*Previous SotA, 625 ps, Keith et al. Phys Rev X (2019) and Thomas et al. Nat Electron (2025)

## Slide 31
A superinductor + IMEC
31

## Slide 32
Multi-module assembly
A superinductor + IMEC
32
Tom Swift
Manuel Suarez
IMEC
Double Quantum Dot
Single-Electron Transistor
\
Width = 0.36 um
Length = 50um
Inductance 140 nH
TiN Kinetic Inductor
Coupling Capacitor
RFin

## Slide 33
Radio-frequency single electron transistor
A superinductor + IMEC
33
Tom Swift
Manuel Suarez
SNR increases linearly with P
SNR increases as P3
Increased sensitivity in the non-linear regime

## Slide 34
A superinductor + IMEC
34
Tom Swift
Manuel Suarez
(4,0)
(3,0)
(4,1)
(3,1)
(NL,NR) = (# e- in left QD, # e-in right QD)
P1 (V)
P2 (V)
Spin Readout Traces for
Pauli Spin Blockade
DQD Tuneup and Spin Readout
99.96% in 19 µs
Spin Readout Infidelity
Spin Readout Fidelity
Name | Readout Fidelity (%) | Time (µs)
Linear | 99.9 | 40
Nonlinear | 99.96 | 19
Non-linear fast | 99.9 | 1
Ref. Constance Laine’s Thesis
Room for improvement:
Increase power -> Further non-linearity
Optimize charge sensing signal -
Integration

## Slide 35
Dispersive charge sensing

## Slide 36
Dispersive charge sensing
The RF single-electron box
Urdampilleta et al, Nat Nano 14 737 (2019)
Borjans et al, Phys Rev App 15 044052 (2021)
Key characteristics:
Measures a single electron ac current between a quantum dot and a charge reservoir
Changes in device impedance (now capacitive) produce a change in the resonance frequency that translates into changes in the magnitude and phase of the reflection coefficient.
sensor

## Slide 37
SEB instead of set
Reducing complexity of sensor
Using dispersive charge sensing (SEB)
Constance Laine
37
Laine et al. arXiv:2505.10435 (2025)/ Nat Sensors in press

## Slide 38
Electrically-tunable tunnel barriers (GBi)
Optimization of rf sensor sensitivity (GBB1)
Optimization of qubit properties (GTB2)
Constance Laine
Laine et al. arXiv:2505.10435 (2025)/ Nat Sensors in press
Reducing complexity of sensor
Using dispersive charge sensing (SEB)
38
SEB instead of set

## Slide 39
Quantum Dot Compact Models
Peri et al. Quantum 8 1294 (2024)
Peri et al. npj Quantum Info 10 224 (2025)
Optimization of rf sensor sensitivity (GBB1)
SEB signal (ΔC)
Charge sensing shift (η)
Constance Laine
Total signal (ηΔC)
SINGLE-ELECTRON BOX READOUT
Electrically-tunable tunnel barriers (GBi)
Optimization of rf sensor sensitivity (GBB1)
Optimization of qubit properties (GTB2)

## Slide 40
SINGLE-ELECTRON BOX READOUT
SNR ~ 3 in 10 µs
3-state classification
Constance Laine
Laine et al. arXiv:2505.10435 (2025)/ Nat Sensors in press
Electrically-tunable tunnel barriers (GBi)
Optimization of rf sensor sensitivity (GBB1)
Optimization of qubit properties (GTB2)

## Slide 41
READOUT FIDELITY
Spin parity readout at state-of-the-art Fm = 99.99% in 200s
Readout fidelity – Spin parity
Fm = 99.9% in 200 s
Fm = 99% in 24s
Model: 3-state Hidden Markov
Optimized SEB
Tuning GTB2
tunesT1 ratios
Constance Laine
Laine et al. arXiv:2505.10435 (2025)/ Nat Sensors in press
Electrically-tunable tunnel barriers (GBi)
Optimization of rf sensor sensitivity (GBB1)
Optimization of qubit properties (GTB2)
Notes: 99.9 % for a readout time of 20 µs and 99 % for 4 µs

## Slide 42
Spin parity readout at state-of-the-art Fm = 99.99% in 200s
Readout fidelity – Spin parity
Fm = 99.9% in 200 s
Fm = 99% in 24s
Model: 3-state Hidden Markov
Optimized SEB
Typical two-state model fails to capture true infidelity
    Concludes long T1s would give you best parity RO
    (when really what you want is a high T1,T-/T1,T0 ratio)
    Underestimates infidelity - more than 4 nines!
Tuning GTB2
tunesT1 ratios
Warning to all doing multi-level readout benchmark!
Constance Laine
READOUT FIDELITY
Laine et al. arXiv:2505.10435 (2025)/ Nat Sensors in press
Notes: 99.9 % for a readout time of 20 µs and 99 % for 4 µs

## Slide 43
STEPS TOWARDS integrated
Single-electron Box + integrated superinductor
    SotA <1 ns minimum integration time
    Optimized tunnel rates to reduce tmin using back-gate
Gorka Aizpurua
Notes: 99.9 % for a readout time of 20 µs and 99 % for 4 µs

## Slide 44
Dispersive RF CASCADE
A mix between SEB+INSITU

## Slide 45
Device topology
QUBITS
SENSOR
Overlapping gate design
3-layer process (polysilicon gates)
Ultralow charge noise (< 0.5 eV/)
Natural silicon
Chittock-Wood et al. Nat Electron (2026)

## Slide 46
charge readout
QUBITS
SENSOR
Dispersive Readout via
Radio-frequency Reflectometry
RFin
RFout
Vigneau et al. App Phys Rev 10 021305 (2023)
Overlapping gate design
3-layer process (polysilicon gates)
Ultralow charge noise (< 0.5 eV/)
Natural silicon
Chittock-Wood et al. Nat Electron (2026)

## Slide 47
charge readout
QUBITS
SENSOR
VG0(V)
VG1(V)
Overlapping gate design
3-layer process (polysilicon gates)
Ultralow charge noise (< 0.5 eV/)
Natural silicon
Jacob
Chiittock-Wood
Chittock-Wood et al. Nat Electron (2026)

## Slide 48
RF single- ELECTRON BOX
(Q1,Q2,Qsensor)
Single reservoir charge sensor
Single-electron AC current is dependent on DQD state – (11) OR (02)
System is projected to charge basis for readout
VG0(V)
VG1(V)
Jacob
Chiittock-Wood
Chittock-Wood et al. Nat Electron (2026)

## Slide 49
RF ELECTRON CASCADE
(Q1,Q2,Qsensor)
Synchronous two-electron process:
(i) Tunneling between dots
(ii) Tunneling from sensor to reservoir
Detects the DQD polarizability (in-situ)
Interdot AC current is amplified by cascade process
(1,1,N)
VG1(V)
VG0(V)
Murphy et al. in preparation
Jacob
Chiittock-Wood

## Slide 50
AMPLIFICATION FACTOR
VG0(V)
VG1(V)
Results in a signal to noise ratio for tint = 10 ms
SNR = 1300
Surpassing the SiMOS SOTA SNR = 4 (West et al Nat Nano 2019)
Jacob
Chiittock-Wood
Notes: We note our T1 is short ~24 us, but having said that, it results in a calculated readout fidelity of 80% in 10 us compared to 74% in 3 ms in the previous state of the art for silicon MOS

## Slide 51
Pauli spin BLOCKADE
VG1(V)
(11)
(20)
Notes: Valley splitting is on excess of 70 ueV

## Slide 52
Exchange Control
Technique from J. Petta et al. Science, 309, 5744 (2005)
VG1(V)
VG0(V)
J tunable over 7-144 MHz
T2* tends to 280 ns at large detuning
Gate Quality factor up to 12
Chittock-Wood et al. Nat Electron (2026)
Notes: B=250 mT

## Slide 53
Rf readout SENSORS
Dissipative
Charge sensing (SET, QPC)
Dispersive
Insitu (DGS)
Charge sensing (SEB)
Cascade

## Slide 54
SUMMARY
M. Fernando Gonzalez Zalba: f.gonzalez@nanogune.eu
Recent Advances in Readout of Semiconductor Spin Qubits
  Superinductors for integrated high-fidelity readout
  Single-electron box reduce sensor footprint and achieve high-fidelity readout
  rf cascade: a new dispersive readout technique

## Slide 55
WELCOME
M. Fernando Gonzalez Zalba: f.gonzalez@nanogune.eu

## Slide 56: Bonus STUFF if useful

## Slide 57
OUR APPROACH
Work with silicon fabs to enable large integration
IMEC’s 300 mm line
Multi-gate MOS process
GlobalFoundries
Integration of Analog, Digital and Quantum Electronics

## Slide 58
GlobalFoundries
Quantum dot work:
Rapid charactersiation of 1024 quantum dot devices using a cryogenic MUX [Nat Electron 8 75 (2025)]
Spin readout structures including rf charge sensors and QDs [arxiv2510.13674, (2025)]
Classical cryoelectronic modules:
MW Multiplexers, Amplifiers, IQ mixers, Filters, Voltage bias DACs, Thermometers
  See Ibberson ICECS 1-4 (2024), Oliveri et al, IEEE Trans App Supercon (2025), Noah APR (2025)
cryoelectronics
Hoxton

## Slide 59
D
G
S
BG
The Device: A Quantum Dot
Few-electron quantum dots (the building block of semicon QC) demonstrated in 22FDX
Thomas et al. Nat Electron 8 75 (2025)
Ibberson et al. ICECS (2024)
At cryogenic temperatures - > Isolated electrons in the silicon channel

## Slide 60
3 mm
‘Bloomsbury’ chip
210 devices available in a single cooldown
How to measure MANY QuDots
Thomas et al. Nat Electron 8 75 (2025)
Rapid readout of 1024 quantum dot devices
Cryogenic multiplexer for time division multiplexing (100x500 um2)
Data extraction at 300 mK and analysis in under 5 min

## Slide 61
IQ demodulator
RF input (400 MHz)
Reflection Coefficient proportional to
changes in device impedance
Radiofrequency reflectometry
Large-Scale Characterisation
The device
Multiplexed
Off-chip Superconducting resonator
Notes: Because quantum dots are high impedance devices we embed them in a resonant matching circuit which we can probe through rf reflectometry. In this instance we designed our resonator to work at 400 MHz and here is an example VNA response. As the transistor is turned on, well above its threshold voltage, the resonance diminishes due to the change in the total impedance.

## Slide 62
The Good, the Bad and the Ugly
Multiple experts labelling sets  Trained neural network to identify different QD qualities with 88% accuracy
Identified best device dimensions

## Slide 63
Spin-dependent tunnelling
Ramped
Read
Empty
(2,1)
(2,0)
(1,0)
(1,1)
Load
VGQ(V)
VGS(V)
Load
Empty
Read
Empty
Read
Spin up
Trace
Spin down
Trace
Spin up
event
Load
Ramped readout at finite magnetic field (B)
Spin Up appears as a blip in read phase
Spin Down no signal in the read phase
Notes: The gate lever

## Slide 65
Quantum Motion team
Leadership
People & Operations
Quantum Hardware
Cloud Engineering
IC Design
IC Validation
Device Modelling
Packaging
Cryogenic Labs
Intelligent Automation
Quantum Algorithms & Theory

## Slide 66
WELCOME TO VISIT US
fernando@quantummotion.tech

## Slide 67
DUT
Radio frequency reflectometry
Signal to noise ratio
= coupling coefficient
= resonator impedance
=> contain resonator losses -> maximise
Measurement rate (SNR=1)*
= Charging energy
= fractional change in resistance
Tsys= noise temperature of system
(intrinsic or amplifier)
Vigneau et al, App Phys Rev 10 021305 (2023)
Signal-to-noise ratio

## Slide 68
Radio frequency reflectometry
Signal to noise ratio
= coupling coefficient
Q0 = internal quality factor
= impedance of resonator
= resonant frequency
Measurement rate (SNR=1)*
= gate capacitance ratio
= drive freq/ tunnel rate ratio
= tunnel/thermal energy ratio
Tsys= noise temperature of system (amplifier)
Vigneau et al, App Phys Rev 10 021305 (2023)
Signal-to noise ratio
DUT

## Slide 69
Rf readout
S
Noffpeak
Nonpeak
Benchmark (minimum integration time):
is the integration time
Dissipative
Charge sensing (SET, QPC)
In-situ (DGS)
Charge sensing (SEB)
Dispersive

## Slide 70
RF readout
Benchmark (minimum integration time):
is the integration time
Dissipative
Charge sensing (SET, QPC)
In-situ (DGS)
Charge sensing (SEB)
Electrical Fidelity
Dispersive

## Slide 71
Spin qubit readout
F. Von Horsting et al. Phys Rev App 21, 044016 (2024)